Welding Standards and Competencies

Welding Technology/Welder (48.0508), Sheet Metal Technology/Sheetworking (48.0506)

Industry Standard: National Center for Construction Education & Research (NCCER) Welding, Levels 1 & 2, 5th edition (2015)

Note: MACTE has approved NCCER Core Curriculum and Welding 1 & 2 as an accepted standard.

Welding, Level 1:

Framework, Duties and Tasks:

- Welding Safety

  - Describe basic welding processes, the welding trade, and training/apprenticeship programs.

    - Describe basic welding processes and the welding trade.

    - Describe NCCER standardized training and explain apprenticeship programs.

  - Identify and describe personal protective equipment (PPE) related to the welding trade.

    - Identify and describe body, foot, and hand protective gear.

    - Identify and describe ear, eye, face, and head protective gear.

  - Identify and describe welding safety practices related to specific hazards or environments.

    - Describe the importance of welding safety and identify factors related to accidents.

    - Describe basic welding safety practices related to the general work area.

    - Describe hot work permits and fire watch requirements.

    - Describe confined spaces and their related safety practices.

    - Identify safety practices related to welding equipment.

    - Identify and describe respiratory hazards, respiratory safety equipment, and ways to ventilate welding work areas.

    - Explain the purpose of SDS/MSDS and how it is used.

- Oxyfuel Cutting

  - Describe oxyfuel cutting and identify related safe work practices.

    - Describe basic oxyfuel cutting.

    - Identify safe work practices related to oxyfuel cutting.

  - Identify and describe oxyfuel cutting equipment and consumables.

    - Identify and describe various gases and cylinders used for oxyfuel cutting.

    - Identify and describe hoses and various types of regulators.

    - Identify and describe cutting torches and tips.

    - Identify and describe other miscellaneous oxyfuel cutting accessories.

    - Identify and describe specialized cutting equipment.

  - Explain how to setup, light, and shut down oxyfuel equipment.

    - Explain how to properly prepare a torch set for operation.

    - Explain how to leak test oxyfuel equipment.

    - Explain how to light the torch and adjust for the proper flame.

    - Explain how to properly shut down oxyfuel cutting equipment.

  - Explain how to perform various oxyfuel cutting procedures.

    - Identify the appearance of both good and inferior cuts and their causes.

    - Explain how to cut both thick and thin steel.

    - Explain how to bevel, wash, and gouge.

    - Explain how to make straight and bevel cuts with portable oxyfuel cutting machines.

  - Performance Tasks:

    - Set up oxyfuel cutting equipment.

    - Light and adjust an oxyfuel torch.

    - Shut down oxyfuel cutting equipment.

    - Disassemble oxyfuel cutting equipment.

    - Change empty gas cylinders.

    - Cut shapes from various thicknesses of steel, emphasizing: straight line cutting, square shape cutting, piercing, beveling, cutting slot

    - Perform washing.

    - Perform gouging.

    - Use a track burner to cut straight lines and bevels.

- Plasma Arc Cutting

  - Explain plasma arc cutting processes and identify related safety precautions.

    - Describe the plasma arc cutting processes.

    - Identify safety practices related to plasma arc cutting.

  - Identify and describe plasma arc cutting equipment.

    - Identify and describe plasma arc power units.

    - Identify and describe plasma arc torches and accessories.

    - Identify and describe plasma arc cutting gases and gas control devices.

  - Describe how to set up, safely operate, and care for plasma arc cutting equipment.

    - Describe how to set up plasma arc cutting equipment and the adjacent work area.

    - Describe how to safely operate plasma arc cutting equipment.

    - Describe how to care for plasma arc cutting equipment.

  - Performance Tasks:

    - Set up plasma arc cutting equipment.

    - Set the amperage and gas pressures or flow rates for the type and thickness of metal to be cut using plasma arc equipment.

    - Square-cut metal using plasma arc equipment.

    - Bevel-cut metal using plasma arc equipment.

    - Pierce and cut slots in metal using plasma arc equipment.

    - Dismantle and store the equipment.

- Air-Carbon Cutting and Gouging

  - Define air-carbon arc cutting and identify the related equipment and consumables.

    - Define air-carbon arc cutting.

    - Identify and describe air-carbon arc cutting equipment.

    - Identify and describe various types of electrodes.

    - Identify safety practices related to air-carbon arc cutting.

  - Describe how to set up, safely operate, and care for air-carbon arc cutting equipment.

    - Describe how to prepare the equipment and work area for air-carbon arc cutting.

    - Describe how to wash and gouge metals.

    - Describe how to care for air-carbon arc cutting equipment.

  - Performance Tasks:

    - Select and install air-carbon arc cutting electrodes.

    - Prepare the work area and air-carbon arc cutting equipment for safe operation.

    - Use air-carbon arc cutting equipment for washing.

    - Use air-carbon arc cutting equipment for gouging.

    - Perform storage and housekeeping activities for air-carbon arc cutting equipment.

- Base Metal Preparation

  - Identify safety practices related to preparing base metals and describe basic cleaning procedures.

    - Identify safety practices related to preparing base metals.

    - Describe the basic properties and types of carbon and stainless steel.

    - Describe basic metal cleaning procedures and concerns.

  - Identify and describe basic weld joint design and types of welds.

    - Identify and describe the loads that are routinely placed on weld joints.

    - Identify and describe the various types of weld joints.

    - Describe a welding procedure specification (WPS) and the information it provides.

  - Describe how to prepare joints for welding.

    - Describe how to mechanically prepare joints for welding.

    - Describe how to thermally prepare joints for welding.

  - Performance Tasks:

    - Mechanically or hand-grind a bevel on the edge of a ¼”- to ¾”-thick mild steel plate (6 to 20 mm metric plate) at 22 ½ degrees.

    - Thermally bevel the edge of a ¼”- to ¾”-thick mild steel plate (6 to 20 mm metric plate) at 22 ½ degrees.

- Weld Quality

  - Identify and describe the various code organizations that apply to welding and their basic elements.

    - Identify the various welding code organizations and their sponsoring organizations.

    - Identify and describe the basic provisions of welding codes.

  - Identify and describe weld discontinuities and their causes.

    - Identify and describe discontinuities related to porosity and inclusions.

    - Identify and describe discontinuities that result in cracking.

    - Identify and describe discontinuities related to joint penetration, fusion, and undercutting.

    - Identify and describe acceptable and unacceptable weld profiles.

  - Describe various non-destructive and destructive weld examination practices.

    - Describe basic visual inspection methods including measuring devices and liquid penetrants.

    - Describe magnetic particle and electromagnetic inspection processes.

    - Describe the radiographic and ultrasonic inspection processes.

    - Describe destructive testing processes.

  - Describe the welder performance testing process.

    - Describe the qualification of welders by position.

    - Describe welder qualification testing to meet American Welding Society (AWS) and American Society of Mechanical Engineers (ASME) requirements.

    - Describe the process for completing a weld test.

  - Performance Task:

    - Perform a visual inspection VT) on a fillet and/or groove weld and complete an inspection report.

- SMAW – Equipment and Setup

  - Identify SMAW-related safety practices and explain how electrical characteristics apply to SMAW.

    - Define SMAW and identify related safety practices.

    - Explain how various current characteristics apply to SMAW.

  - Identify and describe SMAW equipment.

    - Identify and describe various types of SMAW machines.

    - Identify and describe SMAW welding cable and connectors.

    - Identify common tools used to clean a weld.

  - Explain how to set up and start SMAW equipment.

    - Explain how to set up SMAW equipment.

    - Explain how to start, stop, and maintain SMAW equipment.

  - Performance Task:

    - Set up a machine for SMAW.

- SMAW Electrodes

  - Describe the SMAW electrode classification system and how to select the proper electrode for the task.

    - Describe the AWS filler metal specification system and various electrode characteristics.

    - Describe the characteristics of the four main electrode groups.

  - Explain how to select electrodes and describe their proper care and handling.

    - Identify various considerations in the selection of the proper electrode.

    - Describe the proper handling and storage of electrodes.

- SMAW – Beads and Fillet Welds

  - Explain how to prepare for SMAW welding and how to strike an arc.

    - Identify safety practices related to SMAW.

    - Explain how to prepare the area and equipment for welding.

    - Explain how to strike an arc and respond to arc blow.

  - Explain how to successfully complete various types of beads and welds.

    - Explain how to properly restart and terminate a weld pass.

    - Describe the technique required to produce stringer beads.

    - Describe the technique required to produce weave and overlapping beads.

    - Describe the techniques required to produce fillet welds in various positions.

  - Performance Tasks:

    - Set up welding equipment.

    - Strike an arc.

    - Make stringer, weave, and overlapping beads using E6010 and E7018 electrodes.

    - Make corner welds on an angle iron section end welded to a plate coupon.

    - Make fillet welds using E6010 and E7018 electrodes in the specific positions: Flat (1F), Horizontal (2F), Vertical (3F), Overhead (4F)

- Joint Fit-Up and Alignment

  - Identify and describe various types of fit-up and alignment tools.

    - Identify and describe various fit-up gauges and measuring devices.

    - Identify and describe common weldment positioning equipment.

    - Identify and describe various plate alignment tools.

    - Identify and describe various pipe and flange alignment tools.

  - Describe techniques to avoid weldment distortion and describe the roles of codes and specifications.

    - Describe the causes of weld distortion.

    - Describe the techniques and tools used to control weld distortion.

    - Describe the role of codes and specifications in welding procedures and techniques.

  - Performance Tasks:

    - Fit up joints using plate and pipe fit-up tools.

    - Check the joint for proper fit-up and alignment using gauges and measuring devices.

- SMAW – Groove Welds with Backing

  - Identify various types of groove welds and describe how to prepare for groove welding.

    - Identify various types of groove welds and define related terms.

    - Describe how to prepare for groove welding.

  - Describe the technique required to produce various groove welds.

    - Describe the technique required to produce groove welds in the 1G and 2G positions.

    - Describe the technique required to produce groove welds in the 3G and 4G positions.

  - Performance Tasks:

    - Safely set up arc welding equipment for making groove welds.

    - Make flat welds with backing on V-groove joints using E7018 electrodes.

    - Make horizontal welds with backing on V-groove joints using E7018 electrodes.

    - Make vertical welds with backing on V-groove joints using E7018 electrodes.

    - Make overhead welds with backing on V-groove joints using E7018 electrodes.

- SMAW – Open-Root Groove Welds – Plate

  - Identify various types of groove welds and describe how to prepare for groove welding.

    - Identify various types of groove welds and define related terms.

    - Describe how to prepare the work area and plate for groove welding.

  - Describe the technique required to produce various open V-groove welds.

    - Describe the technique required to produce open V-groove welds in the 1G and 2G positions.

    - Describe the technique required to produce open V-groove welds in the 3G and 4G welds.

  - Performance Task:

    - Make open V-groove welds with E6010 and E7018 electrodes in the following positions: Flat (1G) position, Horizontal (2G) position, Vertical (3G) position, Overhead (4G) position.

Welding, Level 2:

- Welding Symbols

  - Identify and interpret welding symbols and their structure.

    - Describe the structure and placement of welding symbols and identify basic symbols.

    - Identify and interpret size and dimension markings for common types of welds.

    - Identify and interpret various supplemental symbols.

    - Identify and interpret less common welding symbols.

  - Performance Task:

    - Identify and interpret welding symbols on an instructor-provided drawing.

- Reading Welding Detail Drawings

  - Describe welding detail drawings and identify basic drawing elements and features.

    - Describe the object views used to depict welding details.

    - Identify basic drawing elements related to welding detail drawings.

  - Identify and explain how to interpret dimensional information, notes, and a bill of materials.

    - Identify and explain how to interpret dimensional information.

    - Identify and explain how to interpret notes and bill of materials.

  - Performance Task:

    - Draw or sketch a welding drawing based on an instructor-provided image or object.

- Physical Characteristics and Mechanical Properties of Metal

  - Describe the composition and classification systems for a variety of metals.

    - Describe the composition and classification system for ferrous metals.

    - Describe the composition and classification system for low-alloy steel.

    - Describe the composition and classification system for common-grade stainless steel.

    - Describe the composition and classification system for specialty-grade stainless steel.

    - Describe the composition and classification system for nonferrous metals.

  - Describe the physical and mechanical characteristics of metals and explain how to identify base metals.

    - Describe the physical characteristics of different metals.

    - Describe the mechanical properties of different metals.

    - Explain how to identify base metals in field conditions.

    - Describe metallurgy-related considerations for welding.

  - Identify the common structural shapes of metal.

    - Identify the most common structural steel shapes.

    - Identify different structural beam shapes.

    - Identify pipe and tubing types.

    - Identify other common metal forms, including rebar.

- Preheating and Postheating of Metals

  - Describe the relationship between heat and metal and identify preheating methods.

    - Describe the relationship between heat and metal.

    - Identify and describe methods used to preheat metal prior to welding.

    - Identify and describe devices and products used to measure temperature.

  - Describe interpass temperature control and postheating processes.

    - Describe interpass temperature control.

    - Describe various postheating processes.

  - Performance Task:

    - Preheat base metal to 350̊F (177̊C) and verify preheat using a temperature-indicating device.

- GMAW and FCAW – Equipment and Filler Metals

  - Describe basic GMAW/FCAW processes and related safety practices.

    - Describe basic GMAW/FCAW processes.

    - Identify GMAW/FCAW-related safety practices.

    - Describe the various GMAW metal transfer modes.

    - Describe the FCAW metal transfer process.

  - Describe GMAW and FCAW equipment and describe how to prepare for welding.

    - Identify common GMAW/FCAW welding equipment.

    - Describe power source control considerations.

    - Identify and describe welding cables and terminations.

    - Identify and describe external wire feeders and their controls.

    - Identify and describe GMAW and FCAW guns, contact tips, and nozzles.

    - Identify various shielding gases and their related equipment.

    - Explain how to set up welding equipment for GMAW and FCAW welding.

  - Identify various GMAW and FCAW filler metals.

    - Identify various FMAW filler metals.

    - Identify various FCAW filler metals.

  - Performance Task:

    - Set up GMAW and FCAW equipment with appropriate shielding gases and filler metals.

- GMAW – Plate

  - Identify GMAW-related safety practices and explain how to set up for welding.

    - Describe basic GMAW processes.

    - Identify GMAW-related safety practices.

    - Explain how to safely set up the equipment and work area for welding.

  - Describe equipment control and welding procedures for GMAW and explain how to produce basic weld beads.

    - Describe equipment control and welding techniques related to GMAW.

    - Explain how to produce basic GMAW weld beads.

  - Describe the welding procedures needed to produce proper fillet and V-groove welds using GMAW welding techniques.

    - Describe the welding procedures needed to produce proper fillet welds using GMAW welding techniques.

    - Describe the welding procedures needed to produce proper V-groove welds using GMAW welding techniques.

  - Performance Tasks:

    - Make multiple-pass GMAW-S (short-circuit) fillet welds on carbon steel plate coupons in all four 1F through 4F positions, using solid or composite electrode.

    - Make multiple-pass GMAW-S (short-circuit) V-groove welds on carbon steel plate coupons in all four 1G through 4G positions, with or without backing, using solid or composite electrode.

    - Make multiple-pass GMAW spray-transfer fillet welds on carbon steel plate coupons in both the 1F and 2F positions, using solid or composite electrode.

    - Make multiple-pass GMAW spray-transfer V-groove welds on carbon steel plate coupons in the 1G position, with backing, using solid or composite electrode.

- FCAW – Plate

  - Identify FCAW-related safety practices and explain how to prepare for welding.

    - Describe basic FCAW processes.

    - Identify FCAW-related safety practices.

    - Explain how to safely set up the equipment and work area for welding.

  - Describe equipment control and welding procedures for FCAW and explain how to produce basic welding beads.

    - Describe equipment control and welding techniques related to FCAW.

    - Explain how to produce basic FCAW weld beads.

  - Describe the welding procedures needed to produce proper fillet and V-groove welds using FCAW welding techniques.

    - Describe the welding procedures needed to produce proper fillet welds using FCAW welding techniques.

    - Describe the welding procedures needed to produce proper V-groove welds using FCAW welding techniques.

  - Performance Tasks:

    - Make multiple-pass FCAW-G/GM (gas-shielded) and/or FCAW-S (self-shielded) fillet welds on carbon steel plate coupons in all four 1F through 4F positions.

    - Make multiple-pass FCAW-G/GM (gas-shielded) and/or FCAW-S (self-shjelded) V-groove welds on carbon steel plate coupons in all four 1G through 4G positions, with or without backing.

- GTAW – Equipment and Filler Metals

  - Identify GTAW-related safety practices and describe the electrical characteristics that affect GTAW.

    - Identify GTAW-related safety practices.

    - Describe the electrical characteristics that affect GTAW.

  - Identify and describe GTAW equipment and consumables.

    - Identify and describe GTAW welding machines.

    - Identify and describe GTAW torches.

    - Identify and describe GTAW torch nozzles and electrodes.

    - Identify and describe GTAW shielding gases.

    - Identify and describe GTAW filler metals.

  - Explain how to set up for GTAW welding.

    - Explain how to select and position the welding machine.

    - Explain how to connect and set up the shielding gas flow rate.

    - Explain how to select and prepare the tungsten electrode.

    - Explain how to select and install the nozzle along with the tungsten electrode.

  - Performance Tasks:

    - Select a GTAW shielding gas.

    - Select a GTAW filler metal.

    - Connect the shielding gas and set the flow rate.

    - Select and prepare the tungsten electrode.

    - Break down and reassemble a GTAW torch.

- GTAW – Plate

  - Identify GTAW-related safety practices and explain how to set up for welding.

    - Identify GTAW-related safety practices.

    - Explain how to safely set up the equipment and work area for welding.

  - Describe welding techniques for GTAW and explain how to produce basic weld beads.

    - Describe welding techniques related to GTAW.

    - Explain how to produce basic GTAW weld beads.

  - Describe the welding techniques needed to produce proper fillet and open V-groove welds using GTAW welding techniques.

    - Describe the welding techniques needed to produce proper fillet welds using GTAW.

    - Describe the welding techniques needed to produce proper open V-groove welds using GTAW.

  - Performance Tasks:

    - Build a pad with stringer beads on carbon steel plate coupons in the flat position using GTAW equipment and carbon steel filler material.

    - Perform multiple-pass fillet welds on carbon steel plate coupons in all four 1F through 4F positions, using GTAW equipment and carbon steel filler metal.

    - Perform multiple-pass open V-groove welds on carbon steel plate coupons in all four 1G through 4G positions, using GTAW equipment and carbon steel filler metal.